#### Product Data Sheet

June 2014

##### INTERNATIONAL MASTER

##### FOR PROFESSIONAL USE ONLY

## J2070

| 2K HS Plus Clearcoat P190-6690 |
| --- |
| Product | Description |
| P190-6690 | 2K HS Plus Clearcoat |
| P210-870 | 2K HS Plus Hardener - Express |
| P210-872 | 2K HS Plus Hardener - Fast |
| P210-875 | 2K HS Plus Hardener - Medium |
| P210-877 | 2K HS Plus Hardener - Slow/High Temperature |
| P850-1692/1693/1694/1695 | 2K Low VOC Thinners |
| P850-1491/1492/1493/1494/1495 | 2K Thinners |
| P852-1689 | 2K HS Plus Express Thinner |

Product Description

P190-6690 is a high solids 2-pack acrylic clearcoat.  It offers a hard and durable finish with

superb gloss and is suitable for all types of repair.

The P190-6690 2K HS Plus Clearcoat system offers a full range of processing options, from an 	
Express 10 minutes at 60°C (metal temperature) bake system for the most rapid processing of small
repairs, to a 40 minutes at 60°C metal temperature bake system ideal high temperature application
conditions.

For compliance reasons P190-6690 has been designed for application with HVLP or Compliant
spray guns. It can be used in two modes, standard 2-coat application and "one visit" application,
where 1 light/medium flowing coat is followed by a full coat with no flash-off* between coats.

Substrates/Preparation

P190-6690 should be applied only over: -

- P965-line Aquabase® basecoats
- P989 Aquabase® Plus basecoats

- Prepared existing paintwork in sound condition.  Existing paintwork should first be
  abraded (E.g. with Scotchbrite™ Ultrafine Grey with P562-106) and cleaned with 
   P980-251, P980-9010 or P980-8252 prior to application of P190-6690.

| Standard and Fast Process |
| --- |
|  | Standard and High Temperature Application Systems | Fast System |
|  | P190-6690 3 parts P210-875/-877 1 part P850-16XX or P850-14XX 0.6 parts | P190-6690 3 parts P210-872 1 part P850-16XX or P850-14XX 0.6 part |
|  | 18-20 secs. DIN4 at 20°C | 18-20 secs. DIN4 at 20°C |
|  | Pot life at 20°C: 2-2.5 hours Pot life at 20°C: 1 hour. It is recommended that the clearcoat is activated and thinned just prior to application. With Express systems application should be completed as soon as possible after activation/thinning. |
|  | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Pressure : 0.7 bar/10 psi max ( air cap) | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Pressure : 0.7 bar/10 psi max ( air cap) |
|  | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Inlet Pressure : Refer to spraygun manufacturers instructions, normally 2 bar/30 psi (inlet) | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Inlet Pressure : Refer to spraygun manufacturers instructions, normally 2 bar/30 psi (inlet) |
|  | Conventional 2 coat Process Apply 2 single coats to give 50-75 microns (2-3 thou) dry film thickness Allow 5 -7 mins flash-off between coats. Express Single Visit Process Apply 1 light/medium coat followed by a full coat to give 50 microns (2 thou) dry film thickness. The first coat should be applied to all repair panels before the second coat is applied. For less than 3 panels, allow 2-3 minutes flash between spray coats. For more than 3 panels, no flash off is required. |

| Standard and Fast Process |
| --- |
|  | 0 - 5 minutes flash-off required before baking, depending on oven type | 0 - 5 minutes flash-off required before baking, depending on oven type |
|  | Bake at metal temp. of : P210-875 P210-877 70°C : 20 minutes 25 minutes 60°C : 35 minutes 40 minutes 50°C : 70 minutes 80 minutes Into service : When cool Air-dry (20°C) : Dust free 40-50 mins. 60 minutes Handleable 6 hours 8 hours Into Service : 16 hours 24 hours | Bake at metal temp. of : P210-872 70°C : 15 minutes 60°C : 25 minutes 50°C : 50 minutes Into service : When cool Air-dry (20°C) : Dust free 20-30 mins. Handleable 4 hours Into Service 12 hours |
|  | Short-wave : 8-15 mins full power (depending on colour and equipment) |

| Express and Super Express Process |
| --- |
|  | Express System | Super Express System |
|  | P190-6690 3 parts P210-870 1 part P850-16XX or P850-14XX 0.6 parts | P190-6690 3 parts P210-870/-872 1 part P852-1689 0.6 parts Note: P190-6690 thinned with Express Thinner P852-1689 is not recommended for use over Aquabase® |
|  | 18-20 secs. DIN4 at 20°C | 18-20 secs. DIN4 at 20°C |
|  | Pot life at 20°C : 30-45 mins Pot life at 20ºC: 20 mins It is recommended that the clearcoat is activated and thinned just prior to application. With Express systems application should be completed as soon as possible after activation/thinning. |
|  | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Pressure : 0.7 bar/10 psi max (air cap) | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Pressure : 0.7 bar/10 psi max ( air cap) |
|  | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Inlet Pressure :Refer to spraygun manufacturers instructions, normally 2 bar/30 psi (inlet) | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Inlet Pressure : Refer to spraygun manufacturers instructions, normally 2 bar/30 psi (inlet) |
|  | Conventional 2 coat Process Apply 2 single coats to give 50-75 microns (2-3 thou) dry film thickness Allow 5 -7 mins flash-off between coats. Express Single Visit Process Apply 1 light/medium coat followed by a full coat to give 50 microns (2 thou) dry film thickness. The first coat should be applied to all repair panels before the second coat is applied. For less than 3 panels, allow 2-3 minutes flash between spray coats. For more than 3 panels, no flash off is required. |

| Express and Super Express Process |
| --- |
|  | 0 - 5 minutes flash-off required before baking (depending on oven type) | 0 - 5 minutes flash-off required before baking (depending on oven type) |
|  | Bake at a metal temp. of : 60°C : - 15 minutes 50°C : - 30 minutes Into service : when cool Air-dry (20°C) : Dust free - 20 mins. Handleable - 2 hours Into Service - 8 hours | Bake at a metal temp. of : 60°C : -870/10 minutes, -872/20 minutes 50°C : -870/20 minutes, -872/40 minutes Into service : when cool Air-dry (20°C) : Dust free - 15 - 20 mins Handleable - 1½ - 2 hours Into Service - 6 - 8 hours Depending on hardener used (-870 or –872) |
|  | Short-wave : 8 - 15 mins full power (depending on colour and equipment) |

General Process Notes

FADE-OUT PROCESS P190-6690 2K HS Plus Clearcoat may be faded-out using the Aerosol Fade Out Thinner P850-1622 or Express Blender P273-1106. Please refer to the Fade-out / Blending Processes Technical Data Sheet M1200V for details of the technique to achieve a successful repair. CHOICE OF HARDENER AND THINNER P210-877 Ideal for processing large jobs at very high application temperatures (>34ºC). Gives a 40 minutes at 60°C metal temperature bake system. P210-875 Gives a standard 35 minutes at 60°C metal temperature bake system suitable for all types of job. P210-872 Ideal for faster processing of medium-sized repairs (e.g. up to a front end) giving a 25 Minutes at 60°C metal temperature bake. P210-870 Allows fast processing of small to medium sized jobs, with a 15 minutes at 60°C metal temperature bake time. The choice of thinner should be made according to application temperature, air movement and size of job. The recommendations below are for guidance only :- Thinner : Ideal temperature range : P850-1692/1491/1492 up to 22°C P850-1693/1492/1493 20-32°C P850-1694/1493/1494 above 30°C P850-1695/1495 above 35°C P852-1689 Express Thinner up to 25°C In general use a slower thinner in fast air movement booths, for large jobs and for high temperature application. Use a faster thinner in slow air movement booths, for small jobs and application at cooler temperatures. PAINT TEMPERATURE As with other paint systems, optimum spray application is achieved if the paint is allowed to reach room temperature (20-25°C) before use. This is particularly important for high solids systems. It is strongly recommended that cold paint is warmed to a minimum of 15°C before application. Below this temperature paint application performance may be adversely affected. INFRA-RED DRYING Drying times are dependent upon colour and equipment. Refer to manufacturer's instructions for set-up details. When using Aquabase basecoat, it is particularly important to ensure the basecoat is thoroughly dry before applying the clearcoat. RECOATABILITY P190-6690, in both standard and express modes, is fully recoatable after the "into-service" times.

General Process Notes

RATIOS FOR TEXTURE AND FLEXIBLE OPTIONS The addition of P565-7210/7220 can be used to give a textured finish. For use over flexible substrates, P100-2020 should also be used. Note: The majority of plastics used on cars are considered Rigid. These plastics may have some flexibility when painted off the car, but are rigid once mounted. HS+ Clearcoats only require the addition of the Flexible Additive (See Flexible chart below) when painting very flexible plastics, mostly found on older vehicles, e.g. foam type. The following tables give a 1L weight mix for various topcoat appearances, ready to spray. The weights in grams are cumulative. DO NOT TARE the scale between additions. Guide for using 2K Thinners P850-1491/1492/1493/1494/1495 Substrate Appearance P190-6690 P565-7210 P565-7220 P100-2020 HS Hardener Thinner 14XX Rigid Gloss 639g - - - 870g 988g Fine Textured 287g 641g - - 745g 965g Coarse Textured 392g - 708g - 850g 970g Flexible Gloss 532g - - 635g 867g 984g Fine Textured 210g 522g - 633g 823g 984g Coarse Textured 280g - 506g 654g 908g 994g Guide for using 2K Thinners P850-1692/1693/1694/1695 & P852-1689 Substrate Appearance P190-6690 P565-7210 P565-7220 P100-2020 HS Hardener Thinner 1692/3/4/5 or P852-1689 Rigid Gloss 639g - - - 870g 977g Fine Textured 287g 641g - - 745g 946g Coarse Textured 392g - 708g - 850g 960g Flexible Gloss 532g - - 635g 867g 973g Fine Textured 210g 522g - 633g 823g 970g Coarse Textured 280g - 506g 654g 908g 987g RECTIFICATION AND POLISHING Polishing is not normally required as P190-6690 has a gloss finish. However, if dirt is a problem, denib with P1500 or finer, then polish by machine using a quality polish such as SPP Polishing System (refer to SPP PDS. Polishing of P190-6690 is easiest between 1 and 24 hours after "into service" drying times. PAINTING PLASTICS Use the standard NEXA AUTOCOLOR® plastics painting system (refer to PDS). OTHER POINTS TO NOTE When using 2-pack products it is highly recommended to clean the gun thoroughly immediately after use.

| General Process Notes |
| --- |
| GUIDELINES FOR WEIGHT MIXING Where a specific volume of clearcoat mix is required, this may be best achieved by weight mixing, using the guidelines below. The weights are cumulative - please do NOT tare the scale between additions. |
|  | WEIGHT MIX GUIDE WITH P850-16XX Low VOC THinners & P852-1689 |
| Volume of RFU Paint (Litres) | Weight P190-6690 | Weight P210-870/-872/-875/-877 | Weight P850-1692/1693/1694/1695 or P852-1689 |
| 0.10 L | 64 g | 87 g | 98 g |
| 0.20 L | 128 g | 174 g | 195 g |
| 0.25 L | 160 g | 216 g | 244 g |
| 0.33 L | 211 g | 287 g | 322 g |
| 0.50 L | 320 g | 435 g | 489 g |
| 0.75 L | 479 g | 653 g | 733 g |
| 1.0 L | 639 g | 870 g | 977 g |
| 1.5 L | 959 g | 1305 g | 1466 g |
| 2.0 L | 1278 g | 1740 g | 1954 g |
| 2.5 L | 1598 g | 2175 g | 2443 g |

|  | WEIGHT MIX GUIDE WITH P850-14XX 2K THinners |
| --- | --- |
| Volume of RFU Paint (Litres) | Weight P190-6690 | Weight P210-870/-872/-875/-877 | Weight P850-1491/1492/1493/1494/ 1495 |
| 0.10 L | 64 g | 87 g | 99 g |
| 0.20 L | 128 g | 174 g | 198 g |
| 0.25 L | 160 g | 218 g | 247 g |
| 0.33 L | 211 g | 287 g | 326 g |
| 0.50 L | 320 g | 435 g | 494 g |
| 0.75 L | 479 g | 653 g | 741 g |
| 1.0 L | 639 g | 870 g | 988 g |
| 1.5 L | 959 g | 1305 g | 1482 g |
| 2.0 L | 1278 g | 1740 g | 1976 g |
| 2.5 L | 1598 g | 2175 g | 2470 g |

General Process Notes Best Practices with UHS Products

Paint storage conditions Keep ready for use paint in good conditions to ensure correct viscosity. RFU temperature above a minimum of 15˚C, and ideally over 18˚C. This includes paint, hardeners and thinners. Mixing and making ready for use Activate accurately, and by weight where ever possible. Where mixing must be by volume, only use a round and parallel sided mixing container together with the correct mixing stick. If using a measuring container marked in percentages, you must be sure that the percentages give the correct quantities. Make sure that Hardeners and Thinners are mixed in well. High solids or high viscosity products can take a little longer to mix in, so a good practice is to stir Hardener in first, then add thinner before stirring again. Use mixed product as quickly as possible. Choose the correct Hardener for the required bake cycle. Keep to the recommended levels of additives. Do not exceed the recommended level of additives such as Flexibilisers. Application technique, process and equipment choices Use correct spraygun set ups, and set up the spraygun correctly. Use a “Single Visit” application wherever possible, following the advice given in the application section. Check that the spraybooth is operating effectively. If necessary make an oven check to be sure that metal temperature is reached, especially on low down repair areas. Nexa Autocolor recommendations are based on time at metal temperature, so this should be allowed for in the bake cycle that is set for the job.

These products are for professional use only, and are not to be used for purposes other than those specified. The information on this TDS is based on present scientific and technical knowledge, and it is the responsibility of the user to take all necessary steps in order to ensure the suitability of the product for the intended purpose.

For Heath and Safety information please refer to the material Safety Data Sheet, also available at: www.nexaautocolor.com

For further information please contact:

Customer Service Sales Group

PPG Industries (UK) Ltd

Needham Road

Stowmarket

Suffolk IP14 2AD

Tel:    01449 771771

Fax:   01449 773472