#### Product Data Sheet

June 2014

##### INTERNATIONAL MASTER

##### FOR PROFESSIONAL USE ONLY

## J2570V

| 2K HS Plus Express Clearcoat P190-6659 |
| --- |
| Product | Description |
| P190-6659 | 2K HS Plus Express Clearcoat |
| P210-872 | 2K HS Plus Hardener - Fast |
| P210-875 | 2K HS Plus Hardener - Medium |
| P850-1492/-1493/1494/-1495 | 2K Thinners |
| P850-1692/1693/-1694/-1695 | 2K Low VOC Thinners |
| P852-1689 | 2K HS Plus Express Thinner |

Product Description

P190-6659 is a fast drying high solids 2-pack express clearcoat.  It offers a rapid process for small repairs, and can be used over rigid plastics without the need of a flexible additive.

P190-6659 2K HS Plus Express Clearcoat system comes with a 15 minute bake option at 60°C,

for use on between 1 and 3 panels. There is also a Super Express 10 minute bake option at 60°C

for single panel / spot repair and a Standard 30 minute bake at 60°C option for larger repairs up

to 25°C.  For optimum final appearance the 15 or 30 minute options are recommended depending

on the type of repair.

P190-6659 can be used in two modes, "one visit" application where 1 light/medium flowing

coat is followed by a full coat with no flash-off between coats or a standard 2-coat application

Substrates/Preparation

P190-6659 should be applied only over: -

- P965-line Aquabase® basecoat

- P989-line Aquabase® Plus basecoat

- Prepared existing paintwork in sound condition.  Existing paintwork should first be abraded

(E.g. with Scotch-Brite™ Ultrafine Grey with P562-106) and cleaned with 
   P980-251, P980-9010 or P980-8252 prior to application of P190-6659.

| Process |
| --- |
|  | Super Express System | Express System | Standard System |
|  | P190-6659 3 parts P210-872 1 part P852-1689 0.6 parts Note: P190-6659 thinned with Express Thinner P852-1689 is not recommended for use over Aquabase® | P190-6659 3 parts P210-872 1 part P 850-1492/3/4 or 0.6 parts -1692/3/4 | P190-6659 3 parts P210-875 1 part P 850-1492/3/4/5 or 0.6 parts -1692/3/4/5 |
|  | 18-20 secs. DIN4 at 20°C | 18-20 secs. DIN4 at 20°C | 18-20 secs. DIN4 at 20°C |
| POTLIFE | 20 - 30 minutes at 20°C | 30 - 40 minutes at 20°C | 40 - 50 minutes at 20°C |
|  | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Pressure : 0.7 bar/10 psi max ( @ air cap) |
|  | Fluid Tip Gravity Fed : 1.2-1.4 mm Suction Fed : 1.4-1.6 mm Inlet Pressure : Refer to spraygun manufacturers instructions, normally 2 bar/30 psi (inlet) |
|  | Apply 1 light/medium flowing coat followed by a full coat to give 45 - 50 microns dry film thickness. Apply 2 single coats to give 50-60 microns dry film thickness |
|  | Between coats: - Application 1. 2 - 3 minutes for 1 or 2 panels. Maximum 3 panels no flash off required OR Application 2. 3 -5 mins depending on spraybooth conditions and hardener/thinner combination used. |
|  | 0 - 5 minutes flash-off required before baking, depending on oven type |

| Process |
| --- |
|  | Super Express System | Express System | Standard System |
|  | P210-872 / P852-1689 Bake at metal temp. of 60°C: - 10 minutes Into service : when cool Air-dry (20°C) : Dust free - 20-30 mins. Handleable - 4 hours Into Service - 12 hours | P210-872 / P850-1492/93/94 or1692/1693/1694 Bake at metal temp. of 60°C : - 15 minutes Into service : when cool Air-dry (20°C) : Dust free - 20-30 mins. Handleable - 4 hours Into Service - 12 hours | P210-875/P850-1492/93/94/95 or1692/1693/1694/1695 Bake at metal temp. of 60°C : - 30 minutes Into service : when cool Air-dry (20°C) : Dust free - 30-40 mins. Handleable - 6 hours Into Service - 16 hours |
|  | Short-wave : 8-15 mins full power (depending on colour and equipment) |

General Process Notes

FADE-OUT PROCESS P190-6659 Express Clearcoat may be faded-out using the Aerosol Fade Out Thinner P850-1622 or Express Blender P273-1106. Please refer to the Fade-out / Blending Processes Technical Data Sheet M1200V for details of the technique to achieve a successful repair. CHOICE OF HARDENER AND THINNER P210-872 Ideal for faster processing of panel repairs (e.g. up to 3 panels maximum) giving a 10/15 minute at 60°C metal temperature bake. P210-875 Ideal where optimum appearance is required, at application temperatures up to 25°C, giving a 30 minute at 60°C metal temperature bake. The choice of thinner should be made according to application temperature, air movement and size of job. The recommendations below are for guidance only :- Thinner : Temperature range : Bake Schedule: Standard For optimum gloss and appearance, P850-1492 /1692 below 25°C over larger area repairs P850-1493/94/95 / 1693/94/95 above 25°C 30 minutes at 60°C Express system For optimum gloss and appearance P850-1492 / 1692 below 25°C 15 minutes at 60°C P850-1493 / 1693 above 25°C 15 minutes at 60°C Super Express system For fast panel / spot repairs P852-1689 below 25°C 10 minutes at 60°C In general use a slower thinner in fast air movement booths, for large jobs and for high temperature application. Use a faster thinner in slow air movement booths, for small jobs and application at cooler temperatures. PAINT TEMPERATURE As with other paint systems, optimum spray application is achieved if the paint is allowed to reach room temperature (20-25°C) before use. This is particularly important for high solids systems. It is strongly recommended that cold paint is warmed to a minimum of 15°C before application. Below this temperature paint application performance may be adversely affected. INFRA-RED DRYING Drying times are dependent upon colour and equipment. Refer to manufacturer's instructions for set-up details. When using Aquabase or Aquabase Plus basecoat, it is particularly important to ensure the basecoat is thoroughly dry before applying the clearcoat. RECOATABILITY P190-6659 is fully recoatable after the "into-service" times. RECTIFICATION AND POLISHING Polishing is not normally required as P190-6659 has a gloss finish. However, if dirt is a problem, denib with P1500 or finer, then polish by machine using a quality polish such as SPP Polishing System (refer to SPP PDS). Polishing of P190-6659 is easiest between 1 and 24 hours after "into service" drying times. USE OF P210-870, 2K HS Plus Hardener - Express This Hardener can be used following the Super Express mixing recommendations above, but is only suitable for use below 25°C and on small areas such as small vertical panels or components where a high gloss finish is not required. Pot Life is 15 minutes so this combination must be applied immediately after mixing and equipment must be cleaned as soon as application is finished. Use on larger areas may lead to popping caused by the very fast cure rate. This combination may be baked at 60°C for 10 minutes or air dried for 12 hours. OTHER POINTS TO NOTE When using 2-pack products it is highly recommended to clean the gun thoroughly immediately after use.

General Process Notes

RATIOS FOR TEXTURE AND FLEXIBLE OPTIONS The addition of P565-7210/7220 can be used to give a textured finish. For use over flexible substrates, P100-2020 should also be used. The following tables give a 1L weight mix for various topcoat appearances, ready to spray. The weights in grams are cumulative. DO NOT TARE the scale between additions. Guide for using 2K Thinner P850-14** Substrate Appearance P190-6659 P565-7210 P565-7220 P100-2020 Hardener P210-872 or P210-875 Thinner -1492/ 93/94/95 Rigid Gloss 645g - - - 875g 994g Fine Textured 287g 641g - - 745g 965g Coarse Textured 392g - 708g - 850g 970g Guide for using 2K Low VOC Thinners P850-16** & 2K HS Plus Express Thinner P852-1689 Substrate Appearance P190-6659 P565-7210 P565-7220 P100-2020 Hardener P210-872 or P210-875 Thinner 1692/93/94/95 or 1689 Rigid Gloss 645g - - - 875g 982g Fine Textured 287g 641g - - 745g 946g Coarse Textured 392g - 708g - 850g 960g Note: 2K HS Plus Express Thinner, P852-1689 is not recommended in combination with P210-875 Hardener.

| General Process Notes |
| --- |
| GUIDELINES FOR WEIGHT MIXING Where a specific volume of clearcoat mix is required, this may be best achieved by weight mixing, using the guidelines below. The weights are cumulative - please do NOT tare the balance between additions. |
| WEIGHT MIX GUIDE WITH P850-14** 2K THinners |
| Target Volume of RFU Paint required (Litres) | Weight P190-6659 | Weight P210-872/ 875 | Weight P850-1492/93/94/95 |
| 0.10 L | 65 g | 88 g | 99 g |
| 0.20 L | 129 g | 175 g | 199 g |
| 0.25 L | 161 g | 219 g | 249 g |
| 0.33 L | 213 g | 289 g | 328 g |
| 0.50 L | 323 g | 438 g | 497 g |
| 0.75 L | 484 g | 656 g | 746 g |
| 1.0 L | 645 g | 875 g | 994 g |
| 1.5 L | 968 g | 1312 g | 1492 g |
| 2.0 L | 1291 g | 1750 g | 1989 g |
| 2.5 L | 1613 g | 2187 g | 2486 g |

| WEIGHT MIX GUIDE WITH P850-16**Low VOC or P852-1689 2K THinners |
| --- |
| Target Volume of RFU Paint required (Litres) | Weight P190-6659 | Weight P210-872/875 | Weight P850-1692/1693/1694/1695 Or P852-1689 |
| 0.10 L | 65 g | 88 g | 98 g |
| 0.20 L | 129 g | 175 g | 196 g |
| 0.25 L | 161 g | 219 g | 245 g |
| 0.33 L | 213 g | 289 g | 324 g |
| 0.50 L | 323 g | 438 g | 491 g |
| 0.75 L | 484 g | 656 g | 736 g |
| 1.0 L | 645 g | 875 g | 982 g |
| 1.5 L | 968 g | 1312 g | 1473 g |
| 2.0 L | 1291 g | 1750 g | 1964 g |
| 2.5 L | 1613 g | 2187 g | 2454 g |

Note: 2K HS Plus Express Thinner, P852-1689, is not recommended in combination with P210-875 Hardener.

General Process Notes Best Practices with UHS Products

Paint storage conditions Keep ready for use paint in good conditions to ensure correct viscosity. RFU temperature above a minimum of 15˚C, and ideally over 18˚C. This includes paint, hardeners and thinners. Mixing and making ready for use Activate accurately, and by weight where ever possible. Where mixing must be by volume, only use a round and parallel sided mixing container together with the correct mixing stick. If using a measuring container marked in percentages, you must be sure that the percentages give the correct quantities. Make sure that Hardeners and Thinners are mixed in well. High solids or high viscosity products can take a little longer to mix in, so a good practice is to stir Hardener in first, then add thinner before stirring again. Use mixed product as quickly as possible. Choose the correct Hardener for the required bake cycle. Keep to the recommended levels of additives. Do not exceed the recommended level of additives such as Flexibilisers. Application technique, process and equipment choices Use correct spraygun set ups, and set up the spraygun correctly. Use a “Single Visit” application wherever possible, following the advice given in the application section. Check that the spraybooth is operating effectively. If necessary make an oven check to be sure that metal temperature is reached, especially on low down repair areas. Nexa Autocolor recommendations are based on time at metal temperature, so this should be allowed for in the bake cycle that is set for the job.

VOC Information The EU limit value for this product (product category: IIB.d) in ready to use form is max. 420g/litre of VOC. The VOC content of this product in ready to use form is max. 420g/litre. Depending on the chosen mode of use, the actual ready to use VOC of this product may be lower than that specified by the EU Directive code. Note: Combinations of this product with P565-554, P565-7210 or P565-7220 will produce a paint film with special properties as defined by the EU Directive code. The EU limit for these combinations in ready for use form is 840g/litre of VOC. The VOC content of this product in these combinations is max 840g/L.

These products are for professional use only, and are not to be used for purposes other than those specified. The information on this TDS is based on present scientific and technical knowledge, and it is the responsibility of the user to take all necessary steps in order to ensure the suitability of the product for the intended purpose.

For Heath and Safety information please refer to the material Safety Data Sheet, also available at: www.nexaautocolor.com

For further information please contact:

Customer Service Sales Group

PPG Industries (UK) Ltd

Needham Road

Stowmarket

Suffolk IP14 2AD

Tel:    01449 771771

Fax:   01449 773472