# Text boxes

Before and after any sanding operation, substrates must be thoroughly degreased and sanded.

Substrates:			Preparation:
Bare Steel			P80-P120

Galvanised steel			P400 (dry)

Zintec				Fine sanding pad

Aluminium and alloys		P240-P320(dry)

Electropaint			P320(dry)/P800(wet)

Aged painted surfaces		P240/P320(dry)

GRP , Fibre - glass		P320(dry)

Polyester filler			P80-P120-P180(dry)

PRODUCT DESCRIPTION

PREPARATION

SUBSTRATES PREPARATION

| MIXING USING HARDENER 1.956.9313 | SANDABLE SURFACER | ISOLATOR | WET ON WET SPOT REPAIR |
| --- | --- | --- | --- |
| MIXING RATIO | VOLUME WEIGHT | VOLUME WEIGHT | VOLUME WEIGHT |
| EPOXY PRIMER 2104 | 3 100g | 3 100g | 3 100g |
| EPOXY HARDENER 9313 | 1 20.7g | 1 20.7g | 1 20.7g |
| THINNER 2205 | 0.8 15.8g | 1.7 33.7g | 1 19.8g |
| VISCOSTY-DIN4 20° C. | 23 - 25" | 16 - 20" | 21 - 23" |
| POT LIFE | 4 hours @ 20° C | 4 hours @ 20° C | 3 hours @ 20° C |

| MIXING USING HARDENER 1.956.9314 | SANDABLE SURFACER | ISOLATOR | WET ON WET SPOT REPAIR |
| --- | --- | --- | --- |
| MIXING RATIO | VOLUME WEIGHT | VOLUME WEIGHT |  |
| EPOXY PRIMER 2104 | 3 100g | 3 100g | Not Recommended |
| EPOXY HARDENER 9314 | 1 20.7g | 1 20.7g |  |
| THINNER 2205 | 1 15.8g | 1.7 33.7g |  |
| VISCOSTY-DIN4 20° C. | 27 - 29" | 16 - 20" |  |
| POT LIFE | 4 hours @ 20° C | 4 hours @ 20° C |  |

Epoxy Primer 2104 is a 2K Epoxy Surfacer with multiple modes of use.  
It is light grey in colour, chromate-free and has good corrosion resistance over bare metal.
Epoxy Primer 2104  has good adhesion to a wide variety of suitably prepared substrates.  
These include bare and galvanised steel, aluminium, painted surfaces and fillers.
Epoxy Primer 2104  has two dedicated hardeners - together forming a versatile package.

Hardener 9313  offers three modes of use - As a sanding filler, an isolator/sealer under 2K primers & surfacers or as a wet-on-wet for small spot repairs & rub-throughs.
Performance Hardener 9314  gives warranty capability as a sanding filler and can also be used as an isolator/sealer under 2K primers & surfacers.

May 2018     				These products are for professional use only				   Page 1 of 4

|  | SANDABLE SURFACER | ISOLATOR | WET ON WET |
| --- | --- | --- | --- |
| Spray gun set up Gravity spray gun (mm) Number of coats Pressure at the gun (bar) | 1,4 -1,6 1 Light + 2 Full See manufactures recommendations | 1,3 - 1,4 1 Light + 1 Full See manufactures recommendations | 1,3 - 1,4 1 Light + 1 Full See manufactures recommendations |
| Flash of at 20° C. Between coats Before Primer or Topcoat | 5 - 10 min. After Dry & sanding | 5 – 10 min. *Using 9313 10-20 min *Using 9314 20-30 min | 5 – 10 min. *10 minutes |
| *Note: | * If Multiprime is to be used on top of Epoxy Primer 2104 in Isolator or Spot Repair mode – then a minimum of 30mins flash off should be given. |
| Drying Time # Through dry @ 20° C Through dry @ 60° C. Through Dry IR (MW) | Overnight 30mins 10mins | na na na | na na na |
| Dry film thickness | 100-120 Microns |  |  |

# Stoving times are for quoted metal temperature. Additional time should be allowed in the stoving schedule to allow metal to reach recommended temperature.

The drying time for IR is based on a MW lamp & depends on the equipment & lamp to panel distance.
These times are for guidance only.

Note: Gravity spraygun recommended.

HARDENERS - THINNERS

HARDENER 9313	1.956.9313	Hardener for Epoxy Primer 2104

HARDENER 9314	1.956.9314	Performance Hardener 9314

THINNER 2205                   1.911.2205	Thinner for Epoxy Primer 2104

APPLICATION - FLASH OFF AND DRYING

May 2018     				These products are for professional use only				   Page 2 of 4

PERFORMANCE AND LIMITATIONS

May 2018    				These products are for professional use only				   Page 3 of 4

Waterborne Degreaser

AquaMax Precleaner 4501 is a waterborne product suitable for the easy removal of grease, oils, silicone, waxes, dirt and other contaminating agents from old paintwork, bare metal, plastics and any other paintable substrates.

AquaMax Precleaner 4501 has been designed to reduce organic solvent emissions to the atmosphere, and is compliant to forthcoming international legislation.

AquaMax

Precleaner

1.931.4501

Epoxy Primer 2104 must be used with the specified hardeners + thinner
Epoxy Primer 2104 should not be used at temperatures lower than 10°C and humidity higher than 80%.

In filler mode - Epoxy Primer 2104 must be sanded after drying prior to pre-cleaning &  the application of topcoat. When used in Isolator or wet-on-wet spot repair mode Epoxy Primer 2104 must be recoated 
within 8 hours.  After use, clean all equipment thoroughly with cleaning solvent or thinner.

RECOATABILITY

|  | SANDABLE SURFACE | ISOLATOR or SPOT REPAIR |
| --- | --- | --- |
| Sanding Overcoat/Recoat | P360 or finer for Direct Gloss P400 or finer for Basecoat. AQUAMAX®, Aquamax Extra or UHS DURALIT® Extra Direct Gloss | Overcoat with any MaxMeyer® 2K primer or AQUAMAX®, Aquamax Extra or UHS DURALIT® Extra Direct Gloss |

MIXING BY WEIGHT

| PAINT VOLUME (L) | SANDABLE SURFACER MODE. Mixing 3:1:0.8 |
| --- | --- |
|  | 0.20 L | 0.40 L | 0.60 L | 0.80L | 1.00 L |
| Primer | 185.0 | 370.0 | 555.0 | 740.0 | 925.0 |
| Hardener 9313 | 223.3 | 446.7 | 670.0 | 893.3 | 1116.7 |
| Thinner | 252.7 | 505.3 | 758.0 | 1010.7 | 1263.3 |
| PAINT VOLUME (L) | SANDABLE SURFACER MODE. Mixing 3:1:1 |
|  | 0.20 L | 0.40 L | 0.60 L | 0.80L | 1.00 L |
| Primer | 177.6 | 355.2 | 532.8 | 710.4 | 888.0 |
| Hardener 9314 | 214.4 | 428.8 | 643.2 | 857.6 | 1072.0 |
| Thinner | 249.6 | 499.2 | 748.8 | 998.4 | 1248.0 |

| PAINT VOLUME (L) | ISOLATOR MODE Mixing 3:1:1.7 |
| --- | --- |
|  | 0.20 L | 0.40 L | 0.60 L | 0.80L | 1.00 L |
| Primer | 155.8 | 311.6 | 467.4 | 623.2 | 778.9 |
| Hardener 9313/9314 | 188.1 | 376.1 | 564.2 | 752.3 | 940.4 |
| Thinner | 240.6 | 481.1 | 721.7 | 962.2 | 1202.8 |
| PAINT VOLUME (L) | SPOT REPAIR WET-ON-WET MODE Mixing 3:1:1 |
|  | 0.20 L | 0.40 L | 0.60 L | 0.80L | 1.00 L |
| Primer | 177.6 | 355.2 | 532.8 | 710.4 | 888.0 |
| Hardener 9313 | 214.4 | 428.8 | 643.2 | 857.6 | 1072.0 |
| Thinner | 249.6 | 499.2 | 748.8 | 998.4 | 1248.0 |

TECHNICAL DATA

For further information please contact:

PPG Industries (UK) Limited. MaxMeyer Division Customer Service & Sales Group, Needham Road, Stowmarket, Suffolk. IP14 2AD, England.  Tel: 01449 771779  Fax: 01449 773495

May 2018    				These products are for professional use only				   Page 4 of 4

Pack size		1 Ltr primer – 0.33 Ltr hardeners – 1Ltr thinner.

Storage			In a cool dry place away from heat

AquaMax®, Duralit®,  MaxMeyer® and the MaxMeyer logo are trademarks of PPG industries Ohio, Inc.  Copyright  © 2018 PPG Industries Ohio, Inc. All rights reserved.
Copyright in the above product numbers that are original is asserted by
PPG Industries Ohio, Inc.

VOC INFOMATION

The EU limit for this product (product category:IIB.c) in ready for use form is max. 540g/litre Of VOC.  The VOC content of this product in ready for use form is max. 540 g/litre. Depending on the chosen mode of use, the actual ready to use VOC of this product may be lower than that specified by the EU Directive code.

These products are for professional use only and are not to be used for purposes other than those specified.

The information on this TDS is based on present scientific and technical knowledge, and it is the responsibility of the user to take all necessary steps in order to ensure the suitability of the product for the intended purpose.

For Health and Safety information, please refer to the material Safety Data Sheet, also available at: www.maxmeyer.com

SAFETY AND HANDLING